**PRODUCT SPECIFICATION – SECTION 09510 – ACOUSTICAL CEILING PANELS****ConceptZ tm Mineral Fiber Base: Digitally applied pattern on mineral fiber acoustical ceiling panel**

**2.1 MANUFACTURER**

1. Bluffview Development Group LLC: Aspens Design Legacy
2. Address: La Crosse, WI 54603
3. Phone Number: +1 (608) 518 6085
4. Website:[www.interiorsystems.com](http://www.interiorsystems.com)
5. Email: customercare@bluffviewgroup.com

**2.2 ACOUSTIC CEILING UNITS**

A. Acoustical Ceiling Panel (ACP) - [Type ACP-1]

* + 1. Name: Digitally Printed Acoustical Ceiling Panels
		2. Physical Characteristics
			1. Pattern: [Driftwood Planks] [Whitewashed Planks] [Medium Cherry] [Custom]
			2. Size: 23.75’’x 23.75’’
			3. Thickness: 0.750
			4. Edge: Square Lay-In
			5. Finished Surface: Fine Texture
			6. Finished Surface Color: Digitally Printed 4C UV Coating
			7. Core Composition: Wet-felted mineral fiber
			8. Recycled Content: 69%
		3. Performance Criteria
			1. Noise Reduction Coefficient (NRC): 0.75
			2. Ceiling Attenuation Class (CAC): 35
			3. Flame Spread Classification: Class A
				1. Flame Spread 25 or less
				2. Smoked Developed 50