
**PRODUCT SPECIFICATION – SECTION 09510 – ACOUSTICAL CEILING PANELS****ConceptZ tm Mineral Fiber Base: Digitally applied pattern on mineral fiber acoustical ceiling panel**

**2.1 MANUFACTURER**

1. Bluffview Development Group LLC: Aspens Design Legacy
2. Address: La Crosse, WI 54603
3. Phone Number: +1 (608) 518 6085
4. Website:[www.interiorsystems.com](http://www.interiorsystems.com)
5. Email: [customer](mailto:ceilings@interiorsystems.com)care@bluffviewgroup.com

**2.2 ACOUSTIC CEILING UNITS**

A. Acoustical Ceiling Panel (ACP) - [Type ACP-1]

* + 1. Name: Digitally Printed Acoustical Ceiling Panels
    2. Physical Characteristics
       1. Pattern: [Driftwood Planks] [Whitewashed Planks] [Medium Cherry] [Custom]
       2. Size: 23.75’’x 23.75’’
       3. Thickness: 0.750
       4. Edge: Square Lay-In
       5. Finished Surface: Fine Texture
       6. Finished Surface Color: Digitally Printed 4C UV Coating
       7. Core Composition: Wet-felted mineral fiber
       8. Recycled Content: 69%
    3. Performance Criteria
       1. Noise Reduction Coefficient (NRC): 0.75
       2. Ceiling Attenuation Class (CAC): 35
       3. Flame Spread Classification: Class A
          1. Flame Spread 25 or less
          2. Smoked Developed 50