**PRODUCT SPECIFICATION – SECTION 095 10 – ACOUSTICAL CEILING PANELS  
Contouratm : [23¾” x 23¾”] [23¾” x 47¾”] x [3/4”] mineral fiber acoustical ceiling panels with scoring and edges as indicated and specified on drawings**

**2.1 MANUFACTURER**

1. Bluffview Development Group LLC: Aspens Design Legacy
2. Address: La Crosse, WI 54603
3. Phone Number: +1 (608) 518 6085
4. Website:[www.interiorsystems.com](http://www.interiorsystems.com)
5. Email: [customer](mailto:ceilings@interiorsystems.com)care@bluffviewgroup.com

**2.2 ACOUSTIC CEILING UNITS**

A. Acoustical Ceiling Panel (ACP) - [Type ACP-1]

1. Name: Contoura Mineral Fiber Ceiling Panels
2. Physical Characteristics
3. Pattern: [WingWave, WingStraight, RippleWave, RippleMark, RippleFlow]
4. Size: 23.75’’x 23.75’’
5. Thickness: 0.75’’
6. Edge: [Reveal 9/16’’, Reveal 15/16’’]
7. Finished Surface: Lightly Textured lay-in panels. Surface Scoring varied by pattern Finished Surface
8. Finished Surface Color: [White, Standard Flat (Manila, Beige Breeze, Haze, Platinum), Metallic, Custom Flat Latex Color #]
9. Core Composition: Wet-felted mineral fiber
10. Recycled Content: 68%

3. Performance Criteria

a. Noise Reduction Coefficient (NRC): 0.50

b. Ceiling Attenuation Class (CAC): 35

c. Flame Spread Classification: Class A Non-combustible

* + - * 1. Flame Spread 25
        2. Smoked Developed 50

