**PRODUCT SPECIFICATION – SECTION 095 10 – ACOUSTICAL CEILING PANELS  
Slatetm : [23¾” x 23¾”] [23¾” x 47¾”] x [5/8”] mineral fiber acoustical ceiling panels with High Ceiling Attenuation Class Rating (CAC 45)**

**2.1 MANUFACTURER**

1. Bluffview Development Group LLC: Aspens Design Legacy
2. Address: La Crosse, WI 54603
3. Phone Number: +1 (608) 518 6085
4. Website:[www.interiorsystems.com](http://www.interiorsystems.com)
5. Email: [customer](mailto:ceilings@interiorsystems.com)care@bluffviewgroup.com

**2.2 ACOUSTIC CEILING UNITS**

A. Acoustical Ceiling Panel (ACP) - [Type ACP-1]

* + 1. Name: Slate Mineral Fiber Acoustical Ceiling Panels
    2. Physical Characteristics
       1. Pattern: Fine Stone
       2. Size: 23.75’’x 23.75’’
       3. Thickness: 0.630’’
       4. Edge: Square, Reveal, Narrow Reveal
       5. Finished Surface: Lightly Textured lay-in panels
       6. Finished Surface Color: [White, Standard Flat (Manila, Beige Breeze, Haze, Platinum), Metallic, Custom Flat Latex Color #]
       7. Core Composition: Slate Embossed wet-felted mineral fiber
       8. Recycled Content: 31%
    3. Performance Criteria
       - 1. Noise Reduction Coefficient (NRC): 0.15
         2. Ceiling Attenuation Class (CAC): 42
         3. Flame Spread Classification: Class A Non-combustible

Flame Spread 25

Smoked Developed 50

