**PRODUCT SPECIFICATION – SECTION 095 10 – ACOUSTICAL CEILING PANELS
Slatetm : [23¾” x 23¾”] [23¾” x 47¾”] x [5/8”] mineral fiber acoustical ceiling panels with High Ceiling Attenuation Class Rating (CAC 45)**

**2.1 MANUFACTURER**

1. Bluffview Development Group LLC: Aspens Design Legacy
2. Address: La Crosse, WI 54603
3. Phone Number: +1 (608) 518 6085
4. Website:[www.interiorsystems.com](http://www.interiorsystems.com)
5. Email: customercare@bluffviewgroup.com

**2.2 ACOUSTIC CEILING UNITS**

A. Acoustical Ceiling Panel (ACP) - [Type ACP-1]

* + 1. Name: Slate Mineral Fiber Acoustical Ceiling Panels
		2. Physical Characteristics
			1. Pattern: Fine Stone
			2. Size: 23.75’’x 23.75’’
			3. Thickness: 0.630’’
			4. Edge: Square, Reveal, Narrow Reveal
			5. Finished Surface: Lightly Textured lay-in panels
			6. Finished Surface Color: [White, Standard Flat (Manila, Beige Breeze, Haze, Platinum), Metallic, Custom Flat Latex Color #]
			7. Core Composition: Slate Embossed wet-felted mineral fiber
			8. Recycled Content: 31%
		3. Performance Criteria
			- 1. Noise Reduction Coefficient (NRC): 0.15
				2. Ceiling Attenuation Class (CAC): 42
				3. Flame Spread Classification: Class A Non-combustible

Flame Spread 25

Smoked Developed 50

